${QR}

Attention to: ﻣﺆﺳﺴﺔ ﻋﻨﻴﻔﻪ ﺳﻠﻴﻤﺎﻥ ﺑﻦ ﻋﻠﻴﺎﻥ ﺍﻟﺮﺷﻴﺪﻱ ﻟﻠﻤﻘﺎﻭﻻﺕ ﺍﻟﻌﺎﻣﺔ

IDI PR #: 123111

Established by: Amr Yasser

# TIS Visit

# Inspection Report - Soil Improvement

Date of visit: 26-Jan-2025

Location: 26.2676204,50.0230492

( Special Projects, Saudi Arabia)

| Owner | ﺿﻴﻒ ﺍﻟﻠﻪ ﺑﻦ ﻣﺤﻤﺪ ﺑﻦ ﻣﺜﻌﻲ ﺍﻟﻌﺘﻴﺒﻲ | TIS Company | CPV Arabia |
| --- | --- | --- | --- |
| Contractor | ﻣﺆﺳﺴﺔ ﻋﻨﻴﻔﻪ ﺳﻠﻴﻤﺎﻥ ﺑﻦ ﻋﻠﻴﺎﻥ ﺍﻟﺮﺷﻴﺪﻱ ﻟﻠﻤﻘﺎﻭﻻﺕ ﺍﻟﻌﺎﻣﺔ | Report Issue Date |  |
| Project Location | ﺍﻟﻘﻄﻌﺔ ﺭﻗﻢ 701 ﻣﺨﻄﻂ 92*6 ﺍﻟﻤﻨﺘﺰﺓ ﺭﺍﺱ ﺗﻨﻮﺭ | Inspection # | 1 |
| Inspection Stage | Soil Improvement | No. Of buildings | 1 |
| Inspector Name | Amr Yasser | Work in progress | Soil Improvement |
| Email | ayasser@cpvarabia.com | Telephone | 594037209 |

Inspection Results: RD5 WI

Description of the inspections carried out: CPV ARABIA has conducted an on-site technical inspection (IDI) for Project PR #123111 during the pre-pouring phase of the Soil Improvement. The details of the inspection are described further as we go through this report.

Summary

Risks Assessment: - The load is applied incrementally not as per approved standards (e.g., ASTM D1196). the load is applied incrementally should comply the approved standards (e.g., ASTM D1196). - The compaction test results for the previous layers have not been provided and have not been verified on-site The compaction test results for the previous layers must be provided and verified on-site. Stages missed without TIS involvement: - Not exist Interpretation of Additional Visit: - The test area is not level, not free from debris, and not prepared according to the approved method statement

General Site Pictures and Construction Plans

${GImg}

General site picture and construction plans

Checklist

| No | Checklist | SBC Reference | Result | Remarks |
| --- | --- | --- | --- | --- |
| 1 | Inspection criteria |  |  |  |
| 1.1 | Is the site ready for inspection with safe inspection conditions and safe access for the TIS inspection? | - | Passed |  |
| 1.2 | Were there any modifications in the project that is different from the RD0, Soil Report and Construction Plans...etc.)? | - | Passed |  |
| 1.3 | Is there any missing inspection stages in the project? | - | Passed |  |
| 1.4 | Are there any defects observed that can affect the building’s stability or RD5 inspection for slab stage hasn’t been closed yet? |  | Passed |  |
| 1.5 | Is the laboratory conducting tests certified by an ISO/17025-accredited body? | - | NA |  |
| 2 | Checklist |  |  |  |
| 2.1 | Are there any visible signs of inadequate compaction, such as surface irregularities or material segregation? | - | Passed |  |
| 2.2 | Are the area cleared of debris, vegetation, and loose soil? | - | Passed |  |
| 2.3 | Does the soil classification report been provided and Soil type match the approved specifications? | - | Not Passed |  |
| 2.4 | Are The compaction layer is uniform, and thickness matches with SBC specifications.? | - | Passed |  |
| 2.5 | Do the Compaction equipment and methodology comply with the approved method statement? | - | Passed |  |
| 2.6 | Does the moisture content of the soil match the optimum moisture content (OMC) as per the provided proctor test/modified proctor test results? | - | Passed |  |
| 2.7 | are the Field dry density measured using approved methods (e.g., sand cone, nuclear gauge) as per test specifications? | - | Passed |  |
| 2.8 | Are the compaction test results (Field compaction percentage) satisfactory and comply with SBC? | - | Passed |  |
| 2.9 | Is the test area level, debris-free, and prepared according to the approved method statement? | - | Passed |  |
| 2.10 | Are the load is applied incrementally as per approved standards (e.g., ASTM D1196)? | - | Not Passed |  |
| 2.11 | Are The load-settlement relationship matches design requirements for bearing capacity and settlement limits? | - | Not Passed |  |
| 2.12 | Is a detailed test report, including load-settlement curves and results provided? | - | Passed |  |
| 2.13 | Are the compaction test results for the previous layers provided and verified on site? | - | Passed |  |
| 2.14 | Does the test plate meet the specified dimensions and thickness? | - | Passed |  |

Risk Assessment

The plate diameter and thickness as per test specifications Passed

The compaction test results for the previous layers have been provided and verified on site . Passed

Test report is detailed, including load-settlement curves and results Passed

The load-settlement relationship does not match design requirements for bearing capacity and settlement limits Not Passed

The load is applied incrementally not as per approved standards (e.g., ASTM D1196). Not Passed

The test area is level, free from debris, and prepared according to the approved method statement. Passed

The compaction test results (Field compaction percentage) unsatisfactory and do not comply with SBC Passed

The field dry density measured using approved methods (e.g., sand cone, nuclear gauge) did not comply with the test specifications Passed

The moisture content of the soil is within the optimum moisture content (OMC) based on the provided proctor test results. Passed

The compaction equipment and methodology do not fully comply with the approved method statement. Passed

The compaction layer is not uniform, and its thickness does not conform to SBC specifications. Passed

The soil classification report has been provided, but the soil type does not match the approved specifications. Not Passed

the area cleared of debris, vegetation, and loose soil Passed

There are visible signs of inadequate compaction, such as surface irregularities or material segregation Passed

| Engineer In Charge of Inspection | Area Manager | Technical Inspection Manager |
| --- | --- | --- |
| Name: Amr Yasser | Name: | Name: |
| Signature: | Signature: | Signature: |
| Date of Issuing the report: |  |  |